BAMS for diF:PS

PREVIOUS CONSIDERATIONS

UVO Cleaner  You can find it in the SEM facilities (Down floor, at the enf of the corridor)

MATERIAL

- Semiconductor 2% diF:PS prepared the day before. Preheated in BAMS at 105ºC a couple of hours ago before starting the coatings.

- BAMS bar nº3. It is placed about 30 min – 1h before making the BAMS, previously cleaned (Acetone + IPA + N2 gun).

PROCEDURE

- Clean the substrate with the sonicator. (5 min acetone bath + 5 min IPA bath + N2 gun)

2.	Prepare the SAM solution 20 ml IPA: 40 µl SAM (normally, PFBT)

3.	Place the devices in the UVO cleaner for 25 min.

4.	Immediately place the xips in the SAM solution for 15 min.

5.	Clean with IPA and dry with N2 if used. Those that are not used are kept in IPA.

6.	Place the device and put some CB between the BAMS hotplate and the substrate.

7.	BAMS parameters

- At 10 mm/s there are 2778 motor steps/s

- Deposition on the BAMS of 30-40 uL of SC:PS per device.