ORGANIC SEMICONDUCTOR INK 2% diFT:PS 4:1

PREVIOUS CONSIDERATIONS

The SC dissolution can be used 24 hours after it has been prepared (NOT BEFORE).

MATERIAL

- Spatula for each reagent (one for dIF and other for PS)

- 3 glass vial (normally, of 1.25ml capacity each one)

For PS  Transparent

For the OSC  Amber, because OSC is photosensitive.

Mixture  Amber.

- Polistyrene (PS) of molecular weight (MW) = 10.000 g/mol

- diFT – TES – ADT  OSC

- Chlorobencene as solvent (φ = 1.106 g/ml)

- 2 needles

Big  For Chlorobenzene extration (bottle with Septum)

Small  To use as a septum with the baloon.

- 2 ml syringue

- Baloon with Ar

- Organic Micropipettes (Red and Grey ones)

EQUIPMENT

- Scale (2nd floor)

- Red BAMS at 105ºC

PROCEDURE

- The SC and PS are weighed (see calculations section).

- CB Extraction

2.1 Balloon inflated with argon using the small agulla nailed to the vial.

2.2 With the syringe and the large syringue you extract the CB (NO DOT TAKE THE BOTTLE DOWN).

2.3 Extraction of 2 mL and put it in another glass vial (amber).

3. Dissolve the amount of SC and PS in the corresponding volume of CB. Both vials are recovered with aluminum foil and left on the BAMS at 105º for at least 60 min.

4. Make the mixture following 4:1 proportion (For instance, for a 500ul solution, 400ul must be of OSC and 100ul of PS).

5. Leave the mixture overnight with lower temperature for further use.

CALCULATION

Calculation to have 2% CB weight in PS or SC

To prepare both solution, you need to take in consideration that per each ml of CB there is 22,6 mg de reagent (PS or OSC).

1 mL solution x 1,106 mg CB1 mL solutionx2 g SC/PS100 g CB=0.022 g=22,6 mg

To know the real volume and weight of each reagent:

1) Knowing that each device needs about 30 - 40 µl of CB, the total volume is adjusted according to the number of devices and knowing the ratio of 22.6 the theoretical reagent weight is calculated.

2) The approximate reagent is weighed, and based on the weight obtained, the volume needed to obtain the 2% solution is recalculated.